Rupalox LX

Pad  printing ink for varnished and powder-coated surfaces, ABS, PC, PMMA, PS, as well as some metals

High  gloss,  good opacity,  Single component ink   system  drying   by  oxidation,   very

good printability

Field of Application

Substrates

Rupalox LX is particularly suited to print onto Varnished surfaces Powder-coated surfaces ABS, Polycarbonate (PC) Acrylglas (PMMA) Polystyrol (PS) Some metals

Since all the print substrates mentioned may be different in  printability even  within an individual type,  preliminary trials are essential to  determine the  suitability for  the  intended use.

Characteristics

Drying

Parallel to  physical  surface  drying  (i. e. evaporation of  the  solvents used),  the  actual hardening of the ink film is caused by the oxidative   cross-linking  reaction   between ink

and air oxygen.

Since this drying  process requires  an extended space  of  time,  the  use  of  Rupalox  LX is not recommended for  those  parts  which  have  to packed or post-processed immediately after printing.

Extent of drying	temperature 		time touch-dry 		20 °C	  30 min stackable 		20°C			2 h final hardness 		20°C	2-3 days

The  times  mentioned vary  according  to substrate, depth of cliché, and auxiliaries used. The processing  and curing temperature should not  be lower  than  15°C as irreversible  damage can occur.

All shades are intermixable. Mixing with  other ink  types  or  auxiliaries  must   be  avoided   in order  to maintain the  special characteristics of this outstanding ink range.

Fade resistance

Pigments of medium fade resistance  have been used for the production of Rupalox LX.

Shades  mixed  by adding  overprint varnish  or other  colour shades, and especially white, have a	reduced fade and weather resistance depending on their  mixing  ratio. The fade resistance  also decreases if the printed ink film thickness is  reduced.  The pigments used  are resistant to solvents and plasticizers.

Stress resistance

After proper and thorough drying, the ink film exhibits  outstanding adhesion as well  as rub and scratch resistance. Rupalox LX also displays a good resistance to domestic cleaners.

Lemon Yellow

Golden Yellow

Orange

Scarlet Red

Crimson Red

Magenta

Brown

Violet

Ultramarine  Blue

Royal Blue

Brilliant Blue

Vivid Green

Bright Green

White

Black

Note

Our  technical advice whether spoken,  written, or   through  test   trials   corresponds  to   our current knowledge to  inform about  our products and their  use. This is not meant as an assurance for certain properties of the products nor their suitability for each application.

You  are,  therefore,  obliged  to  conduct  your own   tests   with    our   supplied   products  to confirm their suitability for the desired process or purpose. The selection  and testing  of the ink for specific application is exclusively your responsibility.

Should,  however,  any  liability   claims   arise, they shall be limited to the  value of the goods delivered   by  us   and   utilized   by  you   with respect   to  any  and   all  damages   not   caused intentionally or by gross negligence.