Ruparop PP

Pad printing  ink  for pre-treated  and un-treated polypropylene

Satin  gloss,  good  opacity,  fast  drying Single -component ink system, very flexible

Field of Application

Substrates

Ruparop PP is particularly suited to print onto Pre-treated or untreated polypropylene (PP) Mostly,   a  pre-treatment  of  the   surface   by flaming,   Corona   discharge   or   applying   our Special Primer is not necessary.

Some polypropylene materials  may show lubricant residues  on  the  surface,  due  to  the production, which  can reduce  adhesion of the ink film. In these cases, please check if you can print 	without pre-cleaning without any difficulties.

Since all the print substrates mentioned may be different in  printability even  within an individual type,  preliminary trials are essential to  determine the  suitability for  the  intended use.

Field of use

The satin-gloss and fast drying  Ruparop PP is mainly  used when it is to print  onto  polypro- pylene,  e. g. to decorate  advertising products or to mark injection-moulded parts. Its good adhesion enables  prints onto  many  non  pre- treated  polypropylene materials.

Characteristics

Drying

Physically fast drying. Touch-dry at 20° C after 2-3  min, at 30° C after 30-40 sec. The times mentioned above vary according  to  substrate, depth of cliché, drying conditions, and  the auxiliaries used.

Fade resistance

Only  pigments of high fade resistance  are used in the Ruparop PP range. Shades mixed by adding bronze binder or other colour shades and especially white, have a reduced fade and weather resistance depending on their mixing ratio. The fade resistance also decreases if the printed ink  film  thickness is reduced. The pigments used are resistant to solvents and plasticizers.

Stress Resistance

After  proper  and   thorough  drying,   the   ink film's  surface  has  an  outstanding stability,  is stackable  and  shows   an  excellent   flexibility. The  chemical   resistance   of  Ruparop PP  to hand  perspiration and  abrasion  is rather  low and  also only  slightly  resistant to  mild  fillers containing a max. alcohol solution of 50 %.

Although  it  is  a  physically   drying   ink,  this special binder  achieves its final resistance  only after several days.

Available Basic shades

Lemon yellow

GoldenYellow

Orange

Magenta

Crimson Red

Bright Red

Dark Brown

Vivid Green

Ultramarine Blue

Deep Blue

Royal Blue

Brilliant Green

White

Black

All shades are intermixable. Mixing with  other ink  types  or  auxiliaries  must   be  avoided   in order  to maintain the  special characteristics of this outstanding ink range.

Attention

For  an  ink  mixture  containing retarder, only thinner should be used for additional thinning during the print run.

Recommendation

The ink should be stirred  well before printing. To protect the ink in opened containers against excessive  drying,  it  can  be  carefully  covered with  a layer of thinner which  can then  be later stirred into the ink prior to printing.

Note

Our  technical advice whether spoken,  written, or   through  test   trials   corresponds  to   our current knowledge to  inform about  our products and their  use. This is not meant as an assurance for certain properties of the products nor their suitability for each application.

You  are,  therefore,  obliged  to  conduct  your own   tests   with    our   supplied   products  to confirm their suitability for the desired process or purpose. The selection  and testing  of the ink for specific application is exclusively your responsibility.

Should,  however,  any  liability   claims   arise, they shall be limited to the  value of the goods delivered   by  us   and   utilized   by  you   with respect   to  any  and   all  damages   not   caused intentionally or by gross negligence.